## Slide 1: Ion milling of 100nm-thick Silicon Nitride membrane
Briosne Frejaville Clemence
Mau Adrien

## Slide 2
Figure 1 :
Milling of holes with a ion-column of aperture 10µm and a current of 0.6pA. The total charge goes from 2pC (left) to 4pC (right). We reach holes with diameter around 20nm.
Figure 1
Figure 2 :
Milling of holes with a ion-column of aperture 20µm and a current of 7pA. This is a view from the other side of the hole. The total charge was 2.24pC.
Figure 2

## Slide 3
Figure 3: Milling of hole with a ion-column of aperture 10µm and a current of 0.6pA. This is a view from the other side of the hole. On the unseen side (milled side) the hole is 40nm wide.
Figure 3
FIB milling smallest holes are usually 30nm wide. 20 nm is the best we can achieve but we
can further reduce holes with other processes.

## Slide 4
Figure 4: At the beginning, we had two identical holes. Their diameter was roughly 80 nm. Then, we closed the right hole and reached a 20 nm hole. The shape of the final hole is also more circular.
Figure 4