## Slide 1: Closing holes
10nm
80nm
With SEM we can close holes from both side of the membrane.
frontside
backside

## Slide 2: Closing holes
The size of the hole depends ~linearly of the number of scans

## Slide 3: Profile of line and dot milling
45° view with SEM

## Slide 4: Profile of line and dot milling
SEM at angle revealed the profile of our milling: gaussian or hypergaussian