## Slide 1: FIB Milling of nano-thin SiN membranes
With the supervision of Armandas Balčytis and Saulius Juodkazis
Clémence Briosne-Fréjaville Adrien Mau

## Slide 2: FIB Milling of nano-thin SiN membranes
Focused Ion Beam and membranes
Milling through the membrane
Resolution

## Slide 3: Focused Ion Beam and membranes
Thickness: ~100 nm
Coating: 5 nm Cr
Parameters:
Column: Voltage - Aperture – Current Dot, line and area doses (pC) Number of loops

## Slide 4: Milling through the membrane
We can spot a hole with the contrast, or with the ability of the membrane to fall.
Two kind of designs
Ion beam
Make-fall of a membrane
Use of contrast
Pierced !
Just a scratch

## Slide 5: Milling through the membrane
Detect the breakthrough for holes and lines
Make-fall
Use of contrast

## Slide 6: Milling through the membrane
Remarks:
If the number of loops is increased, we must increase the total charge to mill through.
Some line milling are inhomogeneous:
When we mill a large area, it boosts the milling of the surrounding membrane.
Dot dose to pierce is between 1.2 and 1.6 pC
Line dose is between 1152 and 2304 µC.

## Slide 7: Tests of resolution
Repeatability
Step between dots
Total charge to mill through
Hole size
Not milled through
~ Milled through
Not distinguishable
Distinguishable

## Slide 8: Tests of resolution
1 loop
Milled through for 1,6 pC
200 loops
Milled through for 2,8 pC
20 loops
Milled through for 2,4 pC
Hole size ~ 45 nm at 6,5 pA
SEM

## Slide 9: Conclusion
Next weeks:
Use of SEM
Use the 1 pA column
Change the coating (10 nm Cr)
Milling at angle