## Slide 1: FIB Milling of nano-thin SiN membranes
Clémence Briosne-Fréjaville Adrien Mau
Smallest holes achievable : 20nm
Ability to close holes up to ~10nm
Main results:

## Slide 2
Backside view of a through-hole. On the other side the hole is 40nm wide

## Slide 3: Closing holes
Successive SEM scans can slowly close the holes.
10nm
80nm

## Slide 4: FLIM (fluorescence lifetime imaging microscopy )
50 nm holes
20 nm holes
Step: 500 nm
300 nm
100 nm
10x10 holes

## Slide 5: Repeatability?
Loop: 20 i=6,3pA
Total charge: 0,24pC
Hole size 40nm

## Slide 6: Conclusion
Coming soon:
Change the coating (10 nm Au)
Array of nanoholes for microscope use
We can achieve very small hole size. The challenge is to measure them, and to get a better repeatibility.